Supporting Information for

Amorphous Iridium Oxide Integrated Anode Electrodes with Ultrahigh Material Utilization for Hydrogen Production at Industrial Current Densities

Lei Ding1, #, Kui Li1, #, Weitian Wang1, Zhiqiang Xie1, Shule Yu1, Haoran Yu2, David A. Cullen2, Alex Keane3, Kathy Ayers3, Christopher B. Capuano3, Fangyuan Liu4, Pu-Xian Gao4,5, and Feng-Yuan Zhang1,*

1 Department of Mechanical, Aerospace & Biomedical Engineering, University of Tennessee, Knoxville, TN, 37996, USA

2 Center for Nanophase Materials Sciences, Oak Ridge National Lab, Oak Ridge, TN 37831, USA

3 Nel Hydrogen, Wallingford, CT 06492, USA

4 Institute of Materials Science, University of Connecticut, Storrs, CT 06269, USA

5 Department of Materials Science & Engineering, University of Connecticut, Storrs, CT 06269, USA

# Lei Ding and Kui Li contribute equally to this work.

*Corresponding author. E-mail: fzhang@utk.edu (Feng-Yuan Zhang)

Supplementary Figures and Tables

Fig. S1 Top-view SEM image (A, B) of the TTLGDL with a pore size of 200 m and a porosity of 40%

Fig. S2 (A) SEM-EDS mapping images of IrOx CCLGDL (0.075 mg cm-2); (B) EDS analysis of IrOx CCLGDL (0.075 mg cm-2)

Fig. S3 (A) SEM-EDS mapping images of IrOx CCLGDL (0.170 mg cm-2); (B) EDS analysis of IrOx CCLGDL (0.170 mg cm-2)

Fig. S4 (A) SEM-EDS mapping images of IrOx CCLGDL (0.340 mg cm-2); (B) EDS analysis of IrOx CCLGDL (0.340 mg cm-2)

Fig. S5 XRD pattern of the IrOx/Ti

Fig. S6 XRD pattern of the IrOx/CP

Fig. S7 Cross-section SEM image of the IrOx CCLGDL

Fig S8 (A) Cell polarization curves and related HFR plot of the TTLGDL coupled with full CCM; (B) Ir mass normalized cell polarization curves of the TTLGDL coupled with full CCM

Table S1 EIS fitting parameters derived from Fig. 6C

Fig. S9 HFR plots of IrOx CCLGDL before and after the stability test

Table S2 Cell test property comparison of previously reported PEMECs with different anodes

| Catalysts | Anode fabrication | Catalyst loading (mg cm-2) | Membrane | Voltage (V) at 1 A cm-2 | Voltage (V) at 2 A cm-2 | Mass-specific current at 1.7 V (A mg-1) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.075-based CCLGDL | Electrodeposition | 0.075 | N117 | 1.68 | 1.84 | 15.26 | This work |
| 0.170-based CCLGDL | Electrodeposition | 0.170 | N117 | 1.66 | 1.80 | 7.732 | This work |
| 0.340-based CCLGDL | Electrodeposition | 0.340 | N117 | 1.64 | 1.77 | 4.383 | This work |
| IrO2 (pattern-3) | Commercial/spray | 0.42 | N117 | 1.69 | 1.89 | 2.43 | ACS Appl. Mater. Interfaces 14 (2022) 2335 |
| IrO2 | Adams fusion method/ spray | 2.5 | N117 | 1.75 | / | 0.352 | Applied Surface Science 514 (2020) 145943 |
| IrRuOX | Spray-drying+ calcination/ spray + decal | 1.8 | N115 | 1.67 | 1.85 | 0.711 | Adv. Energy Mater. 9 (2019) 1802136 |
| IrOX | Spray-drying+ calcination/ spray + decal | 2 | N115 | 1.68 | 1.85 | 0.575 | Adv. Energy Mater. 9 (2019) 1802136 |
| IrO2 nanoneedles | Adams’ fusion method/ spray + decal | 4 | N117 | 1.80 | 2.18 | 0.178 | Adv. Funct. Mater. 2028 (2018) 1704796 |
| IrO2 | Hydrothermal reaction/spray | 1.5 | N117 | 1.72 | / | 0.603 | Chem. Eng. J. 419 (2021) 129455 |
| Ir0.7Ru0.3OX (TT) | Wet chemical method/spray | 1 | N212 | 1.74 | / | 0.835 | Nano Energy 34 (2017) 385 |
| IrOX@IrO2 (A-450) | Adams’ fusion method/ spray | 1 | N115 | 1.79 | 2.21 | 0.750 | Electrochim. Acta 390 (2021) 138885 |