Supporting Information for

Fluorine Modulated MXene-derived Catalysts for Multi-Phase Sulfur Conversion in Lithium-Sulfur Battery

Qinhua Gu1,2, Yiqi Cao1,3, Junnan Chen1,2, Yujie Qi1, Zhaofeng Zhai1, Ming Lu1,3,*, Nan Huang1,2, Bingsen Zhang1,2,*

1 Shenyang National Laboratory for Materials Science, Institute of Metal Research, Chinese Academy of Sciences, Shenyang 110016, P. R. China

2 School of Materials Science and Engineering, University of Science and Technology of China, Shenyang 110016, P. R. China

3 The Joint Laboratory of MXene Materials, Key Laboratory of Functional Materials Physics and Chemistry of the Ministry of Education, Key Laboratory of Preparation and Application of Environmental Friendly Materials of the Ministry of Education, Jilin Normal University, Changchun 130103, P. R. China

*Corresponding authors. Email: luming@jlnu.edu.cn (Ming Lu); bszhang@imr.ac.cn (Bingsen Zhang)

Supplementary Figures and Tables

Fig. S1 a XRD pattern of Ti3AlC2. SEM images of b Ti3AlC2 MAX, c multilayer Ti3C2, d TiO/Ti3C2 powders, and e TiO/Ti3C2 powders

Fig. S2 TEM images of a Ti3C2 nanosheets and b TiO/Ti3C2. c HRTEM images of TiO/Ti3C2 (The inset is corresponding to local FFTs)

Fig. S3 XPS spectra of Ti3C2, TiO/Ti3C2, and TiOF/Ti3C2

Fig. S4 XPS spectra of a, d Ti 2p, b, e O 1s, and c, f F 1s for Ti3C2 and TiO/Ti3C2

Fig. S5 EELS spectra of TiOF/Ti3C2

Fig. S6 CV curves of a Ti3C2 and b TiO/Ti3C2 batteries at scan rates from 0.1 to 0.5 mV s-1

Fig. S7 Linear fits of the peak current of a peak Ⅰ, b peak Ⅱ and c peak Ⅲ from CV curves

Fig. S8 SEM images of the Li2S deposition morphology on a TiOF/Ti3C2, b TiO/Ti3C2, and c Ti3C2

Fig. S9 SEM images of the Li2S dissolution morphology on a TiOF/Ti3C2, b TiO/Ti3C2, and c Ti3C2

Fig. S10 CV curves of Ti3C2, TiO/Ti3C2, and TiOF/Ti3C2 batteries

Fig. S11 CV curves at 0.1 mV s−1 with a Ti3C2 and b TiO/Ti3C2 at 40, 50, and 60 °C

Fig. S12 Schematic diagram of the battery assembly for operando Raman spectroscopy.

Fig. S13 Schematic diagram of the battery assembly for operando XRD spectroscopy

Fig. S14 XPS of TiOF/Ti3C2-Li2S6 at different discharge/charge states

Fig. S15 ELF of a TiOF/Ti3C2, b TiO/Ti3C2, and c Ti3C2

Fig. S16 XPS of F 1s on the TiO/Ti3C2-Li2S6 at different discharge/charge states

Fig. S17 Charge/discharge curves of TiOF/Ti3C2 cathodes at different current rates

Fig. S18 Optical photos of separators a with the TiO/Ti3C2 cathode and b with the TiOF/Ti3C2 cathode after 500 cycles at 0.2 C

Fig. S19 SEM images of Li anodes of batteries a with the TiO/Ti3C2 cathode and b with the TiOF/Ti3C2 cathode after 500 cycles at 0.2 C

Fig. S20 Cycling performance with a sulfur mass loading of 6.71 mg cm-2 at 0.05 C

Fig. S21 Li-S battery performance comparison

Table S1 The element content of Ti3C2, TiO/Ti3C2, and TiOF/Ti3C2

| Materials | Ti (at%) | C (at%) | O (at%) | F (at%) |
| --- | --- | --- | --- | --- |
| TiOF/Ti3C2 | 24.06 | 44.96 | 23.63 | 7.36 |
| TiO/Ti3C2 | 21.85 | 40.99 | 32.13 | 5.03 |
| Ti3C2 | 22.19 | 36.76 | 25.89 | 14.25 |

Table S2 Peaks potentials and potential difference from Fig. S10

| Electrode | Reduction peak (R1, R2) (V) | Oxidation peak (O1, O2) (V) |  |
| --- | --- | --- | --- |
| Ti3C2 | 2.31, 2.037 |  | 2.31, 2.378 |
| TiO/Ti3C2 | 2.33, 2.025 |  | 2.295, 2.376 |
| TiOF/Ti3C2 | 2.306, 2.068 |  | 2.308, 2.35 |

Table S3 Bader charge of TiOF/Ti3C2, TiO/Ti3C2, and Ti3C2

|  | TiOF/Ti3C2 | TiO/Ti3C2 | Ti3C2 |
| --- | --- | --- | --- |
| Ti | -1.9409 | -1.1306 | -1.586 |

Table S4 Shift values of binding energy for Li, F, S and Ti at different discharge/charge states

| Potentials | Li (eV) | F (eV) | S (eV) | Ti (eV) |
| --- | --- | --- | --- | --- |
| 2.14 V | 0 | 0 | 0 | 0 |
| 1.7 V | -0.2 | 0.6 | -1.09 | -0.3 |
| 2.42 V | 0 | 0.4 | 1.82 | 0 |
| 2.6 V | 0.2 | 0 | 2.13 | 0.5 |