Supporting Information for

Tailoring Artificial Solid Electrolyte Interphase via MoS2 Sacrificial Thin-Film for Li-Free All-Solid-State Batteries

Dong-Bum Seo1,†, Dohun Kim2,†, Mee-Ree Kim2, Jimin Kwon2, Hyeong Jun Kook3, Saewon Kang1, Soonmin Yim1, Sun Sook Lee1, Dong Ok Shin3, Ki-Seok An1,*, and Sangbaek Park2,*

1Thin Film Materials Research Center, Korea Research Institute of Chemical Technology (KRICT), 141 Gajeong-ro, Yuseong-gu, Daejeon 34114, Republic of Korea

2Department of Materials Science and Engineering, Chungnam National University, Daejeon, 34134, Republic of Korea

3Intelligent Sensors Research Section, Electronics and Telecommunications Research Institute (ETRI), Daejeon, 34129, Republic of Korea

† Dong-Bum Seo and Dohun Kim contributed equally to this work.

* Corresponding authors. E-mail: ksan@krict.re.kr (Ki-Seok An); sb.park@cnu.ac.kr (Sangbaek Park)

Supplementary Figures and Tables

Fig. S1 (a) XRD pattern of prepared Li6PS5Cl electrolyte. (b) Nyquist plots of Li6PS5Cl at RT

Table S1 Electrochemical impedance spectroscopy (EIS) properties of Li6PS5Cl as calculated from the Nyquist plot

| Rbulk (Ω) | RGB (Ω) | Impedance (Ω) | Area (cm2) | Thickness (cm) | Conductivity (mS cm-1) |  |
| --- | --- | --- | --- | --- | --- | --- |
| 299.31 | 37.14 | 336.44 | 0.2826 | 0.171 |  | 1.8 |

Fig. S2 The critical current density (CCD) analysis of (a) SUS and (b) MoS2-15m. (c) The galvanostatic cycling test of MoS2-15m conducted at a current density of 0.5 mA cm−2 with an areal capacity of 1.5 mAh cm−2

Fig. S3 CV curve obtained using a liquid electrolyte with (a) SUS and (b) MoS2-15m

Table 2 Redox reaction voltage value and equation with MoS2 based on liquid electrolyte

| Voltage (V) | Redox reaction equation |
| --- | --- |
| 0.52 | LixMoS2 + 4Li+ + 4e- → 2Li2S + Mo |
| 1.4 | MoS2 + 4Li+ + 4e- → LixMoS2 |
| 1.87 | 2Li+ + 2e- + S → Li2S |
| 1.8 | Mo + 2S → MoS2 |
| 2.31 | Li2S → 2Li+ + 2e- + S |

Fig. S4 (a) Nyquist plots of Li6PS5Cl. (b-c) Nyquist plots of full-cell structures with (b) SUS and (c) MoS2-15m before Li plating. (d-e) Nyquist plots of full-cell structures with (d) SUS and (e) MoS2-15m after Li plating

Table 3 EIS properties of SUS CC and MoS2-15m as calculated from the Nyquist plot

| Structure | Lithium Plating | R Bulk (Ω) | R Grain Boundary (Ω) | R Charge Transfer (Ω) |
| --- | --- | --- | --- | --- |
| SUS ¦ LPSCl ¦ SUS | - | 62.84 | 64.3 | - |
| Cathode ¦ LPSCl ¦ SUS | Before | 57 | 57.42 | 37.1 |
| Cathode ¦ LPSCl ¦ SUS | After | 39.88 | 60.8 | 284.2 |
| Cathode ¦ LPSCl ¦ MoS2 | Before | 65.72 | 41.8 | 1.794 |
| Cathode ¦ LPSCl ¦ MoS2 | After | 54.51 | 47.99 | 112.1 |

Fig. S5 Cycling performance of various samples (SUS, MoS2-3m, MoS2-15m, and MoS2-45m) at a current density of 0.2 C