Supporting Information for

Engineering PtFe/LiO₂ Frontier Orbital Interaction for in Li-O₂ Batteries

Yin Zhou1†, Kun Yin2†, Tian Zhang1†, Dongyu Feng1, Jiapei Li1, Anquan Zhu,1 Dewu Lin1, Pan Xue1, Yu Liu1, Yongyu Liu1, Kai Liu1, Kunlun Liu1, Chuhao Luan1, Huawei Yang2, Hou Chen2, Yagang Yao3, and Guo Hong1,4*

1Department of Materials Science and Engineering & Center of Super-Diamond and Advanced Films, City University of Hong Kong, 83 Tat Chee Avenue, Kowloon, Hong Kong SAR 999077, P. R. China

2School of Chemistry and Materials Science, Shandong Key University Laboratory of High Performance and Functional Polymer, Ludong University, Yantai 264025, P. R. China

3National Laboratory of Solid State Microstructures, College of Engineering and Applied Sciences, Jiangsu Key Laboratory of Artificial Functional Materials, Collaborative Innovation Center of Advanced Microstructures, Nanjing University, Nanjing 210093, P. R. China

4The Shenzhen Research Institute, City University of Hong Kong, Shenzhen 518057, P. R. China

†Yin Zhou, Kun Yin, and Tian Zhang contributed equally to this work.

*Corresponding author. E-mail: guohong@cityu.edu.hk (Guo Hong)

Supplementary Figures and Tables

Fig. S1 a, Optimized configurations of the Pt58Fe42 unit cell. b-d, Optimized configurations of the PtFe (111) (b), (200) (c), and (220) (d) crystal plane

Note: When calculating the surface energy of the Pt58Fe42, we approximated Pt58Fe42 as Pt60Fe40. This approach avoids an excessive number of atoms during the expansion of the crystal plane, thereby reducing computational cost.

Fig. S2 (a) The elemental mappings of Pt and Fe in Pt67Fe33 nanowires. (b) XRD pattern of Pt67Fe33 nanowires. (c) EDX spectra of Pt67Fe33 nanosheets

Fig. S3 (a) The elemental mappings of Pt and Fe in Pt87Fe13nanowires. (b) XRD pattern of Pt76Fe24 nanowires. (c) EDX spectra of Pt76Fe24 nanosheets

Fig. S4 Discharged-charge curves of Pt and Pt58Fe42 electrocatalysts with a limited capacity of 1 mAh/cm2

Fig. S5 The adsorption/desorption isotherm of Pt/C and Pt58Fe42/C

Fig. S6 FTIR spectra of initial and discharged Pt58Fe42

Fig. S7 1H NMR spectra of initial and discharged Pt58Fe42

Fig. S8 13C NMR spectra of initial and discharged Pt58Fe42

Fig. S9 SEM images of 1st discharge Pt cathode

Fig. S10 XRD patterns of initial and discharged Pt cathode

Fig. S11 Raman spectra of initial and discharged Pt cathode

Fig. S12. a, b, Optimized configurations of the Pt unit cell (a) and the Pt (111) crystal plane (b)

Fig. S13 The Nyquist plots of Pt58Fe42 (a) and Pt (b) cathodes at different conditions

Fig. S14 O 1s spectra for Pt58Fe42 cathode

Fig. S15 O 1s spectra for Pt cathode

Fig. S16 The XPS spectra in C 1s region of Pt58Fe42 cathodes at different conditions

Fig. S17 XPS spectra of the Pt58Fe42 in Pt 4f region at different conditions

Fig. S18 XPS spectra of the PtFe in Fe 2p region at different conditions

Fig. S19 XPS spectra of Pt cathode in Li 1s at different states

Fig. S20 XPS spectra of Pt cathode in C 1s at different states

Fig. S21 a, The UV-Vis absorption spectra of TiOSO4 solutions at different Li2O2 capacities. b, The standard curve of various Li2O2 capacities in TiOSO4 solution. c, UV-Vis absorption spectra of TiOSO4 solutions with Pt and Pt58Fe42 electrodes at different states. The yield of lithium peroxide (Li₂O₂) is defined as the measured amount of Li₂O₂ divided by the set discharge capacity (0.8 mAh)

Fig. S22 a-c, XRD patterns (a), Raman spectra (b) and XPS spectra (c) of Pt58Fe42 cathode at initial and 1st discharged state at a limited capacity of 1000 mAh g-1. d, The elemental mapping of Pt and Fe distribution for 10th charged (m) Pt58Fe42 cathode at a limited capacity of 1000 mAh g-1

Fig. S23 SEM images of 200th charged Pt58Fe42 cathode

Fig. S24 XPS spectra of Pt cathode in C 1s at different states

Fig. S25 a, b, ELF of Pt (a) and Pt58Fe42 (b)

Fig. S26 The valence band spectra of Pt and Pt58Fe42 by UPS

Fig. S27 a,b, Density of states (DOS) of Pt 5d orbital for Pt (a) and Pt58Fe42. c,d, Density of states (DOS) of Fe 3d orbital for Fe (c) and Pt58Fe42 (d)

Fig. S28 a, Optimized configurations of Fe, Fe/LiO2*, Fe/Li2O2*, and Fe/2Li2O2*. b, The Gibbs free energy profiles of Pt and Pt67Fe33 at various potentials

Fig. S29 a-c, Optimized structures of Pt/O2*, Pt/Li2O2* and Pt/2Li2O2*

Fig. S30 (a-d) EIS results of Pt58Fe42 cathode at different charge capacities

Fig. S31 (a-d) EIS results of Pt cathode at different charge capacities

Fig. S32 a-d, Arrhenius plots of Pt58Fe42 cathode at different charge capacities

Fig. S33 (a-d) Arrhenius plots of Pt cathode at different charge capacities

Fig. S34 a, b, Optimized structures of Pt67Fe33 (a) and Pt76Fe24 (b). c, d, Density of states (DOS) of Pt 5dz2 orbital for Pt67Fe33 (c) and Pt76Fe24 (d)

Fig. S35 a-c, Adsorption energies of LiO2 on Pt67Fe33 (a), and Pt76Fe24 (b) catalysts

Fig. S36 a, Optimized configurations of Pt67Fe33, Pt67Fe33/LiO2*, Pt67Fe33/Li2O2*, and Pt67Fe33/2Li2O2*. b, The Gibbs free energy profiles of Pt and Pt67Fe33 at various potentials

Fig. S37 a, Optimized configurations of Pt76Fe24, Pt76Fe24/LiO2*, Pt76Fe24/Li2O2*, and Pt76Fe24/2Li2O2*. b, The Gibbs free energy profiles of Pt76Fe24 and Pt76Fe24 at various potentials

Fig. S38 a,b, The element mapping of Pt and Fe elements (a) and EDX spectra (b) of Pt82Fe18. c,d, The element mapping of Pt and Fe elements (c) and EDX spectra (c) of Pt70Fe30. e,f, The element mapping of Pt and Fe elements (e) and EDX spectra (f) of Pt64Fe36

Fig. S39 Discharged-charge curves of Pt64Co36, Pt70Co30, and Pt82Co18 electrocatalysts with a limited capacity of 1000 mAh/g

Fig. S40 a-c, The optimized structures of Pt₆₄Co₃₆ (a), Pt₇₀Co₃₀ (b), and Pt₈₂Co₁₈ (c). d-f, Density of states (DOS) of Pt 5dz2 orbital for Pt₆₄Co₃₆ (d), Pt₇₀Co₃₀ (e), and Pt₈₂Co₁₈ (f)

Fig. S41 a, b, The element mapping of Pt and Cu elements (a) and EDX spectra (b) of Pt78Cu22. c, d, The element mapping of Pt and Cu elements (c) and EDX spectra (d) of Pt68Cu32. e, f, The element mapping of Pt and Co elements (e) and EDX spectra (f) of Pt59Cu41

Fig. S42 Discharged-charge curves of Pt59Cu41, Pt68Cu32, and Pt78Cu22 electrocatalysts with a limited capacity of 1000 mAh/g

Fig. S43 a-c, The optimized structures of Pt59Cu41 (a), Pt68Cu32 (b), and Pt78Cu22 (c). d-f, Density of states (DOS) of Pt 5dz2 orbital for Pt59Cu41 (d), Pt68Cu32 (e), and Pt78Cu22 (f)

Table S1 Surface energy of Pt58Fe42 (111) surface

|  | E=(Es-nEu)/2A |  |
| --- | --- | --- |
| Eslab | -9720.1096 | Ha |
| Ebulk | -2431.253654 | Ha |
| Number of atoms per unit cell | 20 | Piece |
| Number of surface atoms | 80 | Piece |
| Atom ratio | 4 |  |
| Length of PtFe unit cell surface | 17.06 | Å |
| Width of the PtFe unit cell | 14.16 | Å |
| Angle | 109° |  |
| Cross-sectional area | 228.283272 | (Å)2 |
| surface energy | 4.681898213 | J/m2 |

Table S2 Surface energy of Pt58Fe42 (200) surface

|  | E=(Es-nEu)/2A |  |
| --- | --- | --- |
| Eslab | -9720.3110 | Ha |
| Ebulk | -2431.253654 | Ha |
| Number of atoms per unit cell | 20 | Piece |
| Number of surface atoms | 80 | Piece |
| Atom ratio | 4 |  |
| Length of PtFe unit cell surface | 15.84 | Å |
| Width of the PtFe unit cell | 12.67 | Å |
| Angle | 90° |  |
| Cross-sectional area | 200.69 | (Å)2 |
| Surface energy | 5.08687524 | J/m2 |

Table S3 Surface energy of Pt58Fe42 (220) surface

|  | E=(Es-nEu)/2A |  |
| --- | --- | --- |
| Eslab | -9720.131866 | Ha |
| Ebulk | -2431.253654 | Ha |
| Number of atoms per unit cell | 20 | Piece |
| Number of surface atoms | 80 | Piece |
| Atom ratio | 4 |  |
| Length of PtFe unit cell surface | 15.84 | Å |
| Width of the PtFe unit cell | 14.16 | Å |
| Angle | 90° |  |
| Cross-sectional area | 224.29 | (Å)2 |
| Surface energy | 4.743030905 | J/m2 |

Table S4 The detailed parameters for the coin cells

| Parameter | Value |
| --- | --- |
| Area of PtFe cathode | 0.785 cm2 (10 mm diameter) |
| Mass of active materials | 2.34 mg (~3 mg/cm2) |
| PVDF | 0.28 mg |
| Solvent | ~10 mg (10 uL electrolyte) |

Qdischarge = QPM×QAMQPM+QAM(1+rbp+rep)

QPM = 11.2 mAh cm-2/3 mg cm-2=3868 mAh g-1

QAM = 1168 mAh g-1

rbp = 0.28 mg/2.34 mg = 0.117

rep= 10 mg/2.34 mg = 4.273

Qdischarge = 444 mAh g-1

Pt58Fe42energy density ≈ 444.5 mAh g-1× 2.7 V= 1200 Wh kg-1

Table S5 The comparison of charge overpotentials for Pt58Fe42 nanowires with various electrocatalysts

| Catalyst | Overpotentials | Cycle performance | References |
| --- | --- | --- | --- |
| Pt58Fe42 | 0.24 V at 100 mA/cm2 (1 mAh/cm2) | 250 cycles at 0.5 mA/cm2 (1 mAh/cm2) | This work |
| RuO2/MnO2 | 0.25 V at 200 mA/g (500 mAh/g) | 45 cycles at 200 mA/g (500 mAh/g) | ACS Catal. 2018, 8, 7983-7990. |
| Pd/CNT | 0.1 V at 0.05 mA/cm2 (0.5 mAh/cm2) | 50 cycles 0.05 mA cm2 (0.5 mAh/cm2) | ACS Energy Lett. 2019, 4, 2782. |
| Pt | 0.2 V at 200 mA/g (12985 mAh/g) | 70 cycles at 1000 mA g-1 (1000 mAh g-1) | ACS Catal. 2018, 8, 9006-9015. e202201416 |
| HEAPtIr | 0.38 V at 200 mA/g (1000 mAh/g) | 150 cycles at 200 mA/g (1000 mAh g-1) | Angew. Chem. Int. Ed. 2023,62, e202310894 |
| Pd3Pb | 0.45 V at 100 mA/g (1000 mAh/g) | 175 cycles at 500 mA/g (1000 mAh/g) | PNAS 2023, 120, e2301439120 |
| PtIr | 0.33 V at 100 mA/g (1000 mAh/g) | 180 cycles at 500 mA/g (1000 mAh/g) | Angew. Chem. Int. Ed. 2021, 60, 26592 |
| NiRu-HTP | 0.54 V at 500 mA/g (1000 mAh/g) | 200 cycles at 500 mA/g (1000 mAh/g) | J. Am. Chem. Soc. 2022, 144, 23239. |
| PtFec/NC | 0.15 V at 200 mA/g (1000 mAh/g) | 210 cycles at 400 mA/g (1000 mAh/g) | Angew. Chem. Int. Ed. 2024, e202418893 |
| PtAu | 0.36 V at 100 mA/g (1000 mAh/g) | 220 cycles at at 500 mA/g (1000 mAh/g) | Angew. Chem. Int. Ed. 2022, 61, e202201416 |
| LaSr(5TM)O3 | 0.79 V at 100 mA/g (1000 mAh/g) | 226 cycles at 200 mA/g (1000 mAh/g) | ACS Nano 2024, 18, 40, 27804. |

Table S6 Surface energy of Pt (111) surface

|  | E=(Es-nEu)/2A |  |
| --- | --- | --- |
| Eslab | -1921.5854 | Ha |
| Ebulk | -480.5840663 | Ha |
| Number of atoms per unit cell | 4 | Piece |
| Number of surface atoms | 80 | Piece |
| Atom ratio | 16 |  |
| Length of PtFe unit cell surface | 5.57 | Å |
| Width of the PtFe unit cell | 5.57 | Å |
| Angle | 120° |  |
| Cross-sectional area | 26.8675634 | (Å)2 |
| surface energy | 0.380077984 | eV/(Å)2 |
| surface energy | 6.08 | J/m2 |
| surface tension | 6.08 | N/m |

Table S7 Fitted values for the equivalent circuit elements

|  | Rs [Ω] | Rct [Ω] |
| --- | --- | --- |
| Before charge |  |  |
| Pt/C | 45.36 | 71.16 |
| Pt58Fe42/C | 42.46 | 39.32 |
| After 1st discharge |  |  |
| Pt/C | 43.24 | 811.2 |
| Pt58Fe42/C | 47.27 | 115.6 |