# Supporting Information for

Moderately Hydrophobic Polymer Protective Layer Enables Zn (100) Deposition for High Utilization Zinc Anodes

Xiaoming Fan1, Peiyi Wu1*, Yucong Jiao1*

1State Key Laboratory of Advanced Fiber Materials, College of Chemistry and Chemical Engineering, Donghua University, Shanghai 201620, P. R. China

*Corresponding authors. E-mail: wupeiyi@dhu.edu.cn (Peiyi Wu); yucong.jiao@dhu.edu.cn (Yucong Jiao)

Supplementary Figures

Fig. S1 Schematic illustration of the preparation process for the PDMAG@Zn

Fig. S2 Cross-sectional SEM image of PDMAG@Zn

Fig. S3 Contact angle test of bare Zn

Fig. S4 The corresponding spatial distribution maps of PACG and PDMAG

Fig. S5 The XPS spectra of a N 1s and b Zn 2p with PDMAA@Zn and PDMAG@Zn

Fig. S6 Ionic conductivity tests of PACG and PDMAG

Fig. S7 DSC measurements of PDMAG and PACG hydrogels

Fig. S8 The Raman spectra peak fittings of a PACG, b PACG-Zn2+, c PDMAG, and d PDMAG-Zn2+

Fig. S9 The 1H NMR spectra of -CH- in 2 M Zn(OTf)2, PACG-Zn2+, and PDMAG-Zn2+

Fig. S10 FTIR spectra of PACG, PACG-Zn2+, PDMAG, and PDMAG-Zn2+

Fig. S11 XPS spectra of a O 1s and b Zn 2p for PACG-Zn2+ and PDMAG-Zn2+

Fig. S12 Raman spectra for -SO3 stretching with 2 M Zn(OTf)2, PACG-Zn2+, and PDMAG-Zn2+

Fig. S13 Arrhenius curves and the activation energies (Ea)

Fig. S14 The EIS curves of the symmetrical Zn batteries with a bare Zn, b PACG@Zn, and c PDMAG@Zn under the temperatures from 20 to 70 oC

Fig. S15 LSV curves of bare Zn, PACG@Zn, and PDMAG@Zn in 2 M Zn(OTf)2 electrolyte

Fig. S16 Tafel curves of the symmetrical Zn batteries measured with different electrodes

Fig. S17 The LSV curves of a bare Zn and b PACG@Zn in 2 M Zn(OTf)2 (H2O and D2O) electrolytes

Fig. S18 The HER curves of PAM and PDMAA coated on NF substrates at 0.5 M H2SO4 electrolyte

Fig. S19 The ESW curves of bare Zn, PACG@Zn and PDMAG@Zn.

Fig. S20 The HOMO-LUMO energy levels for H2O, CGG, PAM, PDMAA, PACG and PDMAG

Fig. S21 The CV curves of symmetrical Zn batteries with a bare Zn, b PACG@Zn, and c PDMAG@Zn under various scanning rates

Fig. S22 Differential capacitance curves for bare Zn, PACG@Zn, and PDMAG@Zn

Fig. S23 Raman spectra of H2O signals at the electrode/electrolyte interface with different electrodes

Fig. S24 In-situ EC-GC curves during Zn plating at 10 mA cm-2 with a bare Zn, b PACG@Zn, and c PDMAG@Zn

Fig. S25 Faraday efficiency of different Zn electrodes during Zn plating at 10 mA cm-2

Fig. S26 CV curves for Zn nucleation on different electrodes

Fig. S27 SEM images for Zn nucleation on different electrodes

Fig. S28 The in situ EIS curves of symmetrical Zn batteries with different electrodes

Fig. S29 SEM images of the zinc anode with PDMAG layer after deposition under 1 mA cm-2, 10 mA h cm-2

Fig. S30 The Zn2+ transference number measurements for different Zn electrodes

Fig. S31  a The structure of DAAM monomer and b WCA test of PDAMG@Zn

Fig. S32 The Zn2+ transference number measurement for PDAMG@Zn electrode

Fig. S33 The SEM images of bare Zn, PACG@Zn and PDMAG@Zn soaked in 2 M Zn(OTf)2 electrolyte for various days

Fig. S34 Corrosion rate for different Zn electrodes

Fig. S35 The Reservoir-based Zn||Cu batteries for assessing average Zn stripping/plating CE of a bare Zn and b PACG@Zn

Fig. S36 The rate performance of symmetrical Zn batteries with different electrodes at various current densities

Fig. R37 Cross-sectional SEM image of PDMAG@Zn after 500 h cycling at 1 mA cm-2, 1mA h cm-2

Fig. S38 XRD spectra of PDMAG@Zn electrodes after plating at 1 mA cm-2 with different deposition capacities

Fig. S39 AFM images of different electrodes after plating for 1 h at the current density of 10 mA cm-2

Fig. S40 The performance of symmetrical Zn batteries with different Zn electrodes at 3 mA cm-2, 3 mA h cm-2

Fig. S41 The shelving-recovery performance for symmetrical Zn batteries with different Zn electrodes at 1 mA cm-2, 1 mA h cm-2

Fig. S42 The shelving-recovery performance for symmetrical Zn batteries with different Zn electrodes at 5 mA cm-2, 5 mA h cm-2

Fig. S43 The performance of symmetrical PDMAG@Zn battery at 1 mA cm-2, 10 mA h cm-2

Fig. S44 SEM images of plating and stripping sides for PDMAG@Zn surface after different cycles at 1 mA cm-2, 15 mA h cm-2

Fig. S45 The related XRD spectra for PDMAG@Zn after different cycles at 1 mA cm-2, 15 mA h cm-2

Fig. S46 The performance of symmetrical Zn batteries with PDMAG@Zn at a 10 mA cm-2, 5 mA h cm-2 and b 10 mA cm-2, 10 mA h cm-2

Fig. S47 Raman spectra of Zn foil and PDMAG@Zn after 30 cycles at 10 mA cm-2, 10 mA h cm-2

Fig. S48 The cross-sectional SEM images of PDMAG@Zn after 30 cycles at 10 mA cm-2, 10 mA h cm-2

Fig. S49 CV curves of Zn||V2O5 batteries with scan rate of 1 mV s-1

Fig. S50 The EIS curves of Zn||V2O5 batteries

Fig. S51 The rate performance of Zn||V2O5 batteries at different current densities

Fig. S52 The performance for PDMAG@Zn||V2O5 battery with mass loading of 7.3 mg cm-2

Fig. S53 The XPS spectra of Zn||V2O5 batteries with a bare Zn, b PACG@Zn and c PDMAG@Zn after 100 cycles at 5 A g-1

Fig. S54 The self-discharge behavior of batteries with different Zn anodes

Fig. S55 GITT tests of Zn||V2O5 batteries with different Zn anodes

Fig. S56 The cycling performance for PDMAG@Zn||I2 battery at 1 A g-1