Supporting Information for

Dual-Ion Co-Storage via Solvation Structure Tuning Toward Ultrafast and Durable Zinc-Organic Batteries

Si Liu1, Zhifeng Lin1, Yanxia Yu3, *, Haozhe Zhang4, * and Xihong Lu2, *

1 School of Electronic and Information Engineering, School of Environmental and Chemical Engineering, Foshan University, Foshan 528000, P. R. China

2 The Key Lab of Low-carbon Chem & Energy Conservation of Guangdong Province, School of Chemistry, Sun Yat-Sen University, Guangzhou 510275, P. R. China

3 School of Applied Physics and Materials, Wuyi University, Jiangmen 529020, P. R. China

4 Pritzker School of Molecular Engineering, University of Chicago, Chicago, IL 60637, USA

* Corresponding authors. E-mail: yuyx26@mail.sysu.edu.cn (Yanxia Yu); zhhaozhe@uchicago.edu (Haozhe Zhang); luxh6@mail.sysu.edu.cn (Xihong Lu)

S1 Supporting Figures

Fig. S1 GCD profiles of Zn//PTCDA battery at 30 A g−1 within ZC, ZC-4PC, ZC-SPC electrolytes

Fig. S2 3D snapshot of ZC electrolyte obtained from MD simulations and partial enlarged snapshot representing Zn2+ inner solvation structure

Fig. S3 The pH of ZC, ZC-4PC, and ZC-SPC electrolytes

Fig. S4 a) The LSV and b) Tafel plots of ZC and ZC-SPC electrolytes, respectively.

Fig. S5 Contact angle of PTCDA electrode with ZC, ZC-2PC, ZC-4PC, and ZC-SPC electrolytes

Fig. S6 GCD profiles of Zn//PTCDA batteries at 30 A g−1

Fig. S7 GCD profiles of Zn//PTCDA batteries at different current densities within a) ZC and b) ZC-SPC electrolytes

Fig. S8 CV profiles of Zn//PTCDA batteries at current densities of 60 mV s−1 and 80 mV s−1 within ZC-SPC electrolytes

Fig. S9 LSV profiles of Zn//PTCDA batteries measured at a scan rate of 0.5 mV s−1 in ZC-SPC and SPC electrolytes

Fig. S10 a) The measured K and Zn content in the PTCDA discharged state at 30 A g−1. b-d) SEM image and corresponding mapping of the PTCDA cathode in the discharged state at 30 A g−1

Fig. S11 Cycling stability comparison of Zn//PTCDA batteries based on ZC-1PC and ZC-2PC electrolytes

Fig. S12 Cycling stability comparison of Zn//PTCDA batteries with ZC-SPC electrolyte at 30 A g−1

Fig. S13 The GCD curves for Zn// PTCDA with ZC-SPC electrolyte from different cycles

Fig. S14 The EIS of Zn//PTCDA batteries before and after cycling

Fig. S15 The XRD of PTCDA cathode for before and after cycling

Fig. S16 The cycling performance of Zn//PTCDA batteries at a current density of 0.1 A g−1 in the ZC and ZC-SPC electrolytes

Fig. S17 Optical images of ZC and ZC-SPC electrolytes after immersing PTCDA electrodes for 7 days

Fig. S18 Optical images of ZC and ZC-SPC electrolytes after being stored at −20 °C for 72 hours

Fig. S19 The rate performance of Zn//PTCDA batteries with the ZC and ZC-SPC electrolytes at −20 °C

Fig. S20 The EIS of ZC-SPC at room temperature and −20 ℃, respectively

Fig. S21 The measured K content in the PTCDA pristine and discharge state

Fig. S22 The content of Zn before and after sputtering

Fig. S23 SEM image and corresponding EDS elemental mapping of the PTCDA cathode in the discharged state

Fig. S24 a) The CV curves of Zn//PTCDA batteries at different scan rates within ZC electrolytes. b) Log(i) versus log(v) plots of cathodic and anodic currents response at marked peaks in a)

Fig. S25 Contribution ratios of the capacitive-controlled (filled area) and diffusion-controlled (blank area) capacities of Zn//PTCDA for a) ZC-SPC and b) ZC electrolytes at a scan rate of 0.5 mV s−1. c) Bar diagram for contribution ratio between capacitive-controlled capacities and diffusion-controlled capacities at different scan rates

Fig. S26 The calculate diffusion coefficients via EIS of Zn//PTCDA batteries with ZC and ZC-SPC electrolytes, respectively

Fig. S27 EIS curves tested under different temperature of (a) ZC-SPC and (b) ZC electrolytes

Fig. S28 Schematic illustration of the desolvation process of (a) ZC and (b) ZC-SPC electrolytes

Fig. S29 Schematic illustration of the intercalation process of (a) ZC-SPC and (b) ZC electrolytes

S2 Supporting Table

Table S1 Comparison of electrochemical performance of organic materials

| Cathodes |  | Electrolyte composition |  | Capacity (mAh g−1) | Voltage (V) |  |  |  | Rate capacity (mAh g−1) |  | Cycle life | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TRT |  | 2 M ZnSO4 | 170 at 0.1 A g−1 |  |  |  | 0.8 |  | 100 at 2 A g−1 | 61.9%/1000 |  | [S1] |
| TCNAQ |  | 2 M ZnSO4 | 166 at 0.05 A g−1 |  |  |  | 1.2 |  | 55 at 1 A g−1 | 81%/1000 |  | [S2] |
| PO |  | 2 M ZnSO4 | 147 at 0.1 A g−1 |  |  |  | 0.6 |  | 90 at 1 A g−1 | 94%/500 |  | [S3] |
| OAP |  | 3 M Zn(CF3SO3)2 | 129.6 at 0.2 A g−1 |  |  |  | 0.5 |  | / | 85.8%/500 |  | [S3] |
| PPy | PVA–KCl– Zn(CH3COO)2 gel |  | 123 at 1.9 A g−1 |  |  | ~0.8 |  | 60 at 21.5 A g−1 |  | 38%/200 |  | [S4] |  |
| PDpBQ |  | 2 M ZnSO4 | 120 at 0.1 A g−1 |  |  |  | 1.16 |  | 63 at 5 A g−1 | 79%/500 |  | [S5] |
| PTDM |  | 3 M Zn(OTF)2 | 118.3 at 0.1 A g−1 |  |  |  | 1.13 |  | 71.5 at 10 A g−1 | 65.6%/6400 |  | [S6] |
| dNPC |  | 20 m LiTFSI +1 m Zn(TFSI)2 | 109 at 0.05 A g−1 |  |  |  | 1.3 |  | 88 at 0.25 A g−1 | 96%/500 |  | [S7] |
| PDA/CNT |  | 3.3 M ZnSO4 | 85 at 1 A g−1 |  |  |  | 0.9 |  | 42 at 5 A g−1 | 96%/500 |  | [S8] |
| π-PMC |  | 2 M ZnCl2 | 122.9 at 0.2 A g−1 |  |  |  | ~ 0.5 |  | 76.9 at 32 A g−1 | 80.8%/500 |  | [S9] |

Supplementary References

- W. Wang, Y. Tang, J. Liu, H. Li, R. Wang et al., Boosting the zinc storage of a small-molecule organic cathode by a desalinization strategy. Chem. Sci. 14, 9033-9040 (2023). https://doi.org/10.1039/D3SC03435F

- Q. Wang, X. Xu, G. Yang, Y. Liu, X. Yao, An organic cathode with tailored working potential for aqueous Zn-ion batteries. Chem. Commun. 56, 11859-11862 (2020). https://doi.org/10.1039/d0cc05344a

- Z. Tie, S. Deng, H. Cao, M. Yao, Z. Niu et al., A symmetric all-organic proton battery in mild electrolyte. Angew. Chem. Int. Ed. 61, 2115180 (2022). https://doi.org/10.1002/anie.202115180

- J. Wang, J. Liu, M. Hu, J. Zeng, Y. Mu et al., A flexible, electrochromic, rechargeable Zn// PPy battery with a short circuit chromatic warning function. J. Mater. Chem. A 6, 11113-11118 (2018). https://doi.org/10.1039/c8ta03143f

- Wang, J. Xiao, W. Tang, Hydroquinone versus pyrocatechol pendants twisted conjugated polymer cathodes for high-performance and robust aqueous zinc-ion batteries. Adv. Funct. Mater. 32, 2108225 (2022). https://doi.org/10.1002/adfm.202108225

- Y. Wang, S. Qiu, D. He, J. Guo, M. Zhao et al., A high-potential bipolar phenothiazine derivative cathode for aqueous zinc batteries. ChemSusChem 16, 2300658 (2023). https://doi.org/10.1002/cssc.202300658

- U. Mittal, F. Colasuonno, A. Rawal, M. Lessio, D. Kundu, A highly stable 1.3V organic cathode for aqueous zinc batteries designed in situ by solid-state electrooxidation. Energy Storage Mater. 46, 129-137 (2022). https://doi.org/10.1016/j.ensm.2022.01.004

- X. Yue, H. Liu, P. Liu, Polymer grafted on carbon nanotubes as a flexible cathode for aqueous zinc ion batteries. Chem. Commun. 55, 1647-1650 (2019). https://doi.org/10.1039/C8CC10060H

- H. Zhang, Y. Fang, F. Yang, X. Liu, X. Lu, Aromatic organic molecular crystal with enhanced π–π stacking interaction for ultrafast zn-ion storage. Energy Environ. Sci. 13(8), 2515-2523 (2020). https://doi.org/10.1039/D0EE01723J