Supplementary Information for

Size Dependent Gold Nanoparticle Interaction at Nano-Micro Interface Using both Monolayer and Multilayer (Tissue-Like) Cell Models

Darren Yohan1, Charmainne Cruje1, Xiaofeng Lu2, Devika B. Chithrani1, 2, ⃰

1Department of Physics, Ryerson University, 350 Victoria Street, Toronto, ON, Canada, M5B 2K3

2 Keenan Research Centre, Li Ka Shing Knowledge Institute, St. Michael's Hospital, Toronto, ON, Canada

⃰ Corresponding author. E-mail: devika.chithrani@ryerson.ca

Tel.: 416 979 5000 ext. 4115; Fax: 416 979 5000

S1 Characterization of Gold Nanoparticles (GNPs)

We used Dynamic Light Scattering (DLS), Transmission Electron Microscopy (TEM), and UV visible spectroscopy to characterize the size distribution of GNPs used for our experiments.

- TEM images of 20 and 50 nm diameter GNPs

Fig. S1 TEM images of 20 (left) and 50 nm (right) diameter GNPs.

The scale bar represents 100 nm

- Table summarizing the TEM, DLS, and UV data for 20 and 50 nm GNPs

|  | UV abruption Wavelength (nm) | Diameter (nm) TEM | Diameter (nm) DLS |
| --- | --- | --- | --- |
| 20 nm | 520 | 19.5 ± 3.3 | 24.2 ± 0.6 |
| 50 nm | 525 | 52.4 ± 5.2 | 52.6 ± 0.8 |